## Slide 1
TE-MSC-MDT

## Slide 2: 11T_112
Reaction report
N. Bourcey
22/07/2015

## Slide 3: Preparation
Start date: 18/06/2015
End date: 27/06/2015
Heat cycle :
Ramp 25°C/h, hold 48h/210°C
Ramp 50°C/h, hold 48h/400°C
Ramp 50°C/h, hold 50h/640°C

## Slide 4: Instrumentation layout
List of vamas and RRR samples (box before after coil):
V1 – HOC0181AF14V.001
V2 – HOC0181AF11V.001
V3 – HOC0181AF11E.001
5 RRR samples (virgin, extracted)
List of vamas and RRR samples (box after before coil):
V7 – HOC0181AF10V.001
V8 – HOC0181AF10E.001
tc10
tc1
tc2
tc3
tc4
tc8
tc9
INLET
OUTLET

## Slide 5: Furnace program
Online change: +120min
Online change: -60min

## Slide 10: Remarks
No fan
New type N thermocouple calibrated
Error in the gas connection: inlet through the RE side of the coil instead of LE.

## Slide 11
TE-MSC-MDT